Annexture-2          Specification

INVITATION OF BIDS FOR SUPPLY OF CAST IRON RAILWAY SHOULDERS FOR SLEEPERS YARD –DEMATGODA, SRI LANKA

TENDER NO: SDSQ /2020/19/S-2/3

Product Specifications – Cast Iron Shoulders

- Scope

This specification covers the minimum manufacturing and testing requirements of cast shoulders manufactured in spheroidal graphite cast iron. The shoulder provides a rail bearing face to maintain track gauge and housing for the installation of the Rail Fastening Clips.

- Material Specification

National Standards

EN 1563	      grade EN-GJS-500-7

ASTM A536     grade 80/55/06

AS 1831	      grade 500/7

- Quality Assurance Testing

Based on the shoulder manufacturer demonstrating that the production process and associated tests are so controlled that conformity to visual and dimensional requirements are assured.

  - Visual (Surface Irregularities)

Only minor surface irregularities, protrusions or cavities are permitted on the complete shoulders.

Note : Surface oxidation of cast shoulders is a normal condition of supply.  Surface oxidation is not detrimental to the performance of the shoulder or the Rail Fastening assembly.

  - Dimensional Accuracy

All dimensions of ‘as made shoulders’ (before the addition of any coating) must be in accordance with the appropriate drawing (Annexure I).

  - Hardness

Cast shoulder hardness shall be 170 to 240 Brinell.

The method of hardness testing shall be in accordance with BS EN ISO 6506-1, ASTM E 10 or AS 1816.1.

  - Micro Structure

Following parameters should be within the given limit.

Nodularity 	: 90% to 95%

Pearlite     	: 35% to 45%

Form		: V&VI

Ferrite		: 40% to 45%

Cementite	: Nil

- Coating

Where specified, shoulders shall be coated with an approved zinc based corrosion preventive coating.

- Mass

Estimated mass of one shoulder is not less than 1.0 kg.

- Responsibility for Tests

All tests detailed in paragraph 3 are the responsibility of the manufacturer and shall be carried out by the manufacturer or a mutually acceptable independent testing authority.

- Certification

The manufacturer will submit with each batch of shoulders (or order if agreed) a certificate of conformity and associated test results confirming that the shoulders supplied have met the requirements of this specification and conform to the appropriate drawing.